ने.गु. २८:२०४०

NS.28:2040

पहिलो पुनरिक्षण :२०७५/०३/१५

नेपाल गुणस्तर

नेपाली हाते (लोक्ता) कागज

(लेख्नमा तथा टाइप गर्नमा प्रयोग हुने )

Nepal Standard

NEPALI HANDMADE (LOKTA) PAPER

(FOR WRITING AND PRINTING PURPOSE)

नेपाल सरकार

उद्योग बाणिज्य तथा आपूर्ति मन्त्रालय

नेपाल गुणस्तर तथा नापतौल बिभाग

बालाजु,काठमाडौं

Nepal Standard

NEPALI HANDMADE (LOKTA) PAPER

(FOR WRITING AND PRINTING PURPOSE)

  - Scope

This standard prescribes requirements and methods of sampling and test for commonly used types of Nepali Handmade (Lokta) papers for writing and printing purpose.

  - Definition

The forest based raw material "Lokta" is a skin/bark of the Lokta plant - a sapling stick of about 8 to 10 feet in height/length. The word Lokta refers to one of the local botanical species of Daphne Cannabina or Daphne Papyracea - a small woody plant of Laurel family

  - Requirements

3.1. Producers/ manufactures shall declare the raw materials and production technology for making nepali handmade ( Lokta) papers.

3.2. Handmade (lokta) papers shall be of uniform in color and shape, smooth surface, evenly finished and free from specks, holes and other blemishes as per testing method in NS 274 (part 1)

3.3.  While writing on the papers with a pen filled with ink complying with  NS 19-038, ink shall not penetrate from one side of surface to the another side of surface and shall not spread on the surface of the papers.

3.4. While writing with black ink on the papers, the color shall not fade.

3.5. The Nepali handmade (lokta) papers are categorized into five grades

Table:1 Types of Handmade paper categorized

| S.N | Types | Nominal weight (g)/size ( cm) | GSM | Nominal Thickness |
| --- | --- | --- | --- | --- |
| 1. | I | 10/50 X75 | 26 | 75 |
| 2. | II | 15/50 X 75 | 39 | 115 |
| 3. | III | 20/50 X 75 | 52 | 160 |
| 4. | IV | 30/50 X 75 | 78 | 230 |
| 5. | V | 40/50 X 75 | 104 | 300 |

3.6 Moisture Content

The Moisture content for all types of writing and printing handmade papers shall be more than 10%, when tested according to NS 274.

3.7	GSM

No single test result shall vary by more than ±20 percent from GSM mentioned in table-1. Further, the mean of 10 test results shall not vary from the GSM by more than ±10 percent

3.8   Sizes and Tolerance on Size

Trimmed sizes of writing and printing paper and the permissible tolerance on the size shall be in accordance with NS 55-2041, 56-2041

3.9 PH

The pH value for all types of writing and printing papers shall be 6.5 to 8.5.

3.10

The handmade papers shall also comply with the requirements given in Table 2. Method of testing paper shall follow as prescribe in NS 274.

  - Packing and Marking

4.1	The packing of paper· shall be done so as to ensure that the paper is not damaged due to handling and transportation and shall be as agreed to between the purchaser and the suppliers.

4.2	Each package shall be marked with the following particulars:

- GSM in g/m2 of  the  paper,

- Size of the paper,

- Mass in kg/ream (No. of Sheet/ream)

- Lot number,

- Month and year of manufacture, and

  - SAMPLING

Representative samples for test shall be drawn as given in NS…..ISO 186 (Paper and Board- Sampling to determine average quality)

6.      Criterions for Conformity

6.1 A sheet not meeting the relevant requirements for any one or more ·characteristics shall be considered as defective.

6.2 A lot shall be declared as conforming to the requirements of this specification if the number of defective sheets found, does not exceed the acceptance number. This acceptance number is zero for the requirement for GSM (see 3.7) and for all other requirements depends upon the size of the Sample and shall be equal to zero if the size is less than 13 and one if the size is greater than or equal to 13.

Table 2 : Requirements for Handmade papers for writing & printing

| S.No | Type of Grade | Basic Weight g/m2 Min | Brightness % Min. | Opacity % Min. | Breaking length (Meter) Min. | Tear Resistance(mN) Min | Resistance to Feathering |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | I | 26 | 48 | 95 | 3400 | 150 | To be passed |
| 2 | II | 39 |  |  | 3200 | 450 | To be passed |
| 3 | III | 52 |  |  | 3000 | 500 | To be passed |
| 4 | 1V | 78 |  |  | 2900 | 570 | To be passed |
| 5 | V | 104 |  |  | 2800 | 800 | To be passed |